## Slide 2: Ecuación de estado termodinámico para líquidos
Los líquidos, como fluidos en reposo o en movimiento, son incompresibles y ocupan todo el volumen que los contiene. Es decir los cambios de la presión apenas modifican la temperatura y el volumen del fluido. El volumen si depende de la temperatura. La relación entre presión, temperatura y volumen específico para fluidos homogéneos guarda relaciones funcionales de linealidad. Sus calores específicos, conductividad térmica y densidades proveen la información necesaria para aplicar en ellos las leyes de la termodinámica. No se requiere la existencia de una ecuación de estado termodinámico para su estudio.

## Slide 3: Ecuación de estado termodinámico para sólidos
To the solid phase then the relationship between the quantities of EOS(equation of state) becomes more complicated and two new thermodynamic parameters are introduced.
First, the function between temperature and volume is characterized by the volume coefficient of expansion [β ].

## Slide 4: Ecuación de estado termodinámico para sólidos
The relationship between the pressure and volume is described by the isothermal bulk modulus [KT ] – [análogo al módulo de Young en resistencia de materiales]
It is assumed that the stresses are isotopic; therefore, the principal stresses can be identified as the pressure
p = σ1 = σ2 = σ3 .

## Slide 5: Ecuación de estado termodinámico para sólidos
Both the volume coefficient of expansion and the isothermal bulk modulus are pressure and temperature dependent; therefore, it is necessary to know the derivatives of these parameters.
It is generally assumed that beside the introduction of the bulk modulus and the volume coefficient of expansion no additional change is required when a phase of a system changes from gas to solid and that the rest of the thermodynamic equations, work function, state functions can be used without modification for solid phase. This widely held consensus would be considered in details.

## Slide 6: 1ra. Ley de la Termodinámica para sólidos
According to the first law of thermodynamics the internal energy [U] change of a system can be calculated as:
dU =  q +  w =n cv dT – pdV
where q is the heat, supplied to or taken away from the system, w is the mechanical work, done by or(-) on(+) the system, and Cv is the molar heat capacity at constant volume. The internal energy U is a state function. In a closed system the path taken from the initial to the final state should not affect the internal energy change between the initial and the final conditions.
Caution: There are two different conventions regarding how the 1st Law is stated. Our convention will be that  w has a
positive value when we do work on the system (and a negative value when the system does work). Engineers tend to
write the 1st Law as dU =  q –  w and define  w to have a positive value when the system does work

## Slide 7: Funciones termodinámicas de estado y de recorrido. Potenciales termodinámicos y ecuaciones diferenciales de la termodinámica (Maxwell)

## Slide 8: Importancia de la energía libre de Gibbs en el estudio termodinámico del estado sólido
Gibbs free energy (G)
The Gibbs free energy is a function designed to be useful for defining conditions of equilibrium. It is this arameter, G, which allows us to find the equilibrium state of a system by considering only the properties of the system, and not also the properties of its surroundings.
As its name suggests, Gibbs free energy can be thought of as the energy which can be available to do useful work.

## Slide 9: Importancia de la energía libre de Gibbs en el estudio termodinámico del estado sólido